## Slide 1
The Latest up-graded Nano Fiber Tec. &
It’s new applications.
1

## Slide 2: What is The “Electro-Spinning”?
Definition: Process that produces a highly impermeable,
non-woven fabric of submicron fibers by pushing
a millimeter diameter liquid jet through a nozzle
with an electric field after making a polymer solution
(fibrillation of polymer)
Ex) Electro Melt spinning & blown: 0.001~0.00001mm
Dry spinning Fiber : 0.5~1.0mm
2

## Slide 3: The World of Micro & Nano Size
3

## Slide 4
Possible to expand to the wide application beyond previous materials.
Growth rate 10% since 2009, Market scale will be 40 billion by 2030 year..
Main market will be energy storage and filter materials..
Energy Storage
44.0%
Filters
20.6%
Medical
3.8%
Coated Fabrics
5.5%
Cleaners
5.1%
Extremity-environmental
Materials 16.5%
Carbon Fiber
4.5%
< Prospect of world-wide nano Fiber-market >
40 B U$
(2030)
(unit : o.1 BU$)
CAGR 22.7%
Market Prospect of Nano Industry.
CAGR 22.7%
Energy Storage
44.0%
4

## Slide 5: Simple Drawing of E/S
Electro-static polymer sosolution
5

## Slide 6
  Origin of Electro-Spinning Tech.
6

## Slide 7: AVAILABLE POLYMERS IN ELECTRO-SPINNING & ITS SOLVENT
PAN (Poly acrylonitrile) ; DMF –(Hydrophobic)
Cellulose; NMMO:Normal Methyl Morpholine N-Oxide)-Applicated for Tire code
Polyimide; PHENOL(Heat resistant)
Polyamides & Poly aramide : SULFURIC ACID(Heat-resistant)
Poly aniline : SULFURIC ACID(Conductive)
PU (Polyurethane) : DMF(Elastics and Adhesive)
PVA (Poly viny lalcohol) : WATER solubility
PVC, PVDF : DMF(Frame retardance & Hydrophobics)
The others : Natural polymer, Polypeptides(Protein), Collagen
7

## Slide 8
Details of Bio-Polymer and It’s Solvent
Polymer
Polyimides
Polyamic acid
Polyetherimide
Nylon 6 & Nylon 66
Polyaramid
Poly-benzyl-glutamate
Poly(p-phenylene terephthalamide)
Polybenzimidazole
Ultem 1000 (Polyether imide)
Nylon 6-co-Polyimide
Polyacrylonitrile(PAN)
PVDF
Polypropylene
PLA
PVA
Collagen
Chitosan
Phenol
m-cresol
Methylene chloride
Formic Acid
Sulfuric acid
Dimethylformamide
Sulfuric acid
Dimethylacetamide
Chloroform
Formic acid
Dimethylformamide
DMF
Melt in vacuum
DMAc
Water
Water/Acetone
Strong Acid
Solvents
Possibility: CNT with other polymer
Graphene with other polymer
8

## Slide 9
‘Smart performance: each functions are revealed by special conditions
Intelligent Textile → Smart & Eco Friendly Fabrics
‘New High Performance’
Composite Textile→ air-permeable & water proof,
→ Anti-baterial etc..
Bio-mimetic textile → Bionic Functional Fabrics
Nano Fiber Textile
High Performance
Fiber
Synthetic Fibers
Natural Fibers
‘Mass production’
softness • Strength, Durability, Chemical-resistance
‘Basic Performance’
Strength, Handle, Warmth, Permeability
New Synthetic Fibers
‘Hybridization & Composite of nano fiber & textile’
: composite functions-Hybrid-textiles, compact..
Future Trend Of Textile –Fabrics.
9

## Slide 10
Trend of HMT(Hybrid Membrane Nano Tech) and Micro Fiber
10

## Slide 11
  Position of Nano fiber Membrane
11

## Slide 12
  Features of Nano fiber
12

## Slide 13: Size Of Nano-Fibers
Nano fiber with P.E.T 2d Spun-bond
Nano-fiber with Hair
13

## Slide 14
Surface Area & Pore Size Of Nano-Fibers
14

## Slide 15
HV
Drop
Charge
Taylor cone
Jet
Spraying, Splitting, Whipping
Collector
Electrospinning
BASIC PRINCIPLE OF ELECTRO-SPINNING
15

## Slide 16
1
2
Classical E-spin
Multiple Classical E-spin(over 80%)
Methods(Patents) of Electro-Spinnings
16

## Slide 17
3
4
Upward type Classical E-spin
Rolling type Classical E-spin
5
Rolling type Classical E-spin
17

## Slide 18
6
Modified Electro-blown spinning (E co.- D co.-C co.)
18

## Slide 19
HV
HV
F co, A co,T co. etc-
D & C Co-
ELECTRO-SPINNING VS. ELECTRO-BLOWN SPINNING
19

## Slide 20
Current Status of E/S
Technology
Nano-size’s deviations of M/D & C/D
Needed to be guaranteed
Air/Liquid Filters, Sports Wear, Bio-medical, Battery Separator, etc.
Productivity
Quality
Needed multiple nozzles(10,000~30,000) in Mass Production
High Maintenance Cost & expensive fixed cost.
Unstable Process Control and not uniform Fiber Diameter(~ 1µm)
Various conditions by Various Polymers Applications
20

## Slide 21
Nanofiber
Fig. 1 Flying direction of filaments Fig. 2 Stretching of filaments by air speed
Melt-Blown System
Use of Spunbond& Melt-Blown Technology for making
Hybrid-Nano fibers
21

## Slide 22
E-Spinning with Spunbond Melt Blown Tech (Hybrid Tech)
Process : SMN PROCESS, SNS PROCESS, SMNS etc...
Compressor
Extruder
Polymer
Filter
Metering Pump
(Gear-type)
Spin Block & Nozzle
Suction Collector
Ring Blower
Winder Unit
Hot-Air
Heater
22
Eletro -Blown Spinning Technology

## Slide 23
Use of Electro-Melt Blown Spinning
23

## Slide 24
Fiber diameter
100um
10um
1um
100nm
Fiber
Dry spinning
Wet spinning
Melt spinning
Meltblown
Productivity
Microfiber
Nanofiber
Modified melt blown
Islands-in-the-sea
Radial sheath separation
Electro-spinning
Nanofiber
Modified E-Spinning
D CO.
Technology
Features of E/Blown Spinning.
24

## Slide 25
Patented Specially Designed Spin Beam
High Efficiency Electric Discharge Configuration
Precision Aerodynamic Flow Control – Laminar Flow
Post Spinning Carrier Recovery System
Post Spinning High Speed Web Handling System
Re-modified Tech of AES Technology(Aero-dynamic E/S)
(World Top Productivity and Quality)
*

## Slide 26
Distinctiveness of AES(Aerodynamic E-Spinning) Tech.
Technology
World-wide Patent Coverage
Low deviation & Various Applications:
Air/Liquid Filters, Sports Wear, Bio-medical, Battery Separator, etc.
Productivity
Quality
Unprecedented Mass Production Productivity - Demostrated
500~1,000% Increase vs. Competitive Technologies
Low Maintenance Cost
Process Control and Uniform Fiber Diameter(~ 1µm)
Up to 90% Porosity, High Surface Area(5~500 m2/g)
Various Polymers Applicable
*

## Slide 27
Maximized specific surface area
Small & even pore
Flow of pores by nano-fibers is extremely complicated
Minimized diameter
The lower diameter,
the more maximized specific surface area..
Protective clothes for chemical & bio industry
Characters of Nano-web
Materials as~
Bio mimetics
Heat resistant battery separator
Sound-insulations
High performance wipes
Medical (surgical suture,Hemostatic ,
Military
Functions & Applications Of Bio Nano-Web (Sheet)
Cosmetics:Facial mask
High performance Filter
Nano liquid Filter
27

## Slide 28: ex1)Future Bio-Nano-Filter:3-Layers. PLA Spunbond+PLA M/B(no-charging)+Nano PLA(E-Spin:500nm)
Filter | section | M/B weight (No-charging) | E (%) | ↓Pressure Drop(mmaq) | S/B+M/B+(E/S)
Mask | Droplets KF-80 | 25 20 25~30 25 | 30~50 80 | 8 10(95LPM) | 30+20+(1~2) 40+25+(2)
 | KF-94 (KN-95) | 30~35 30 (substrate 40) | 94 | 12(95lpm) | 40+30+(3)
Automobile cabin | O.E.M A/S | 20~25 20 (substrats 60~70) | 65~95 | 0.9~1.0 32LPM | 60+20+(1~2)
 | For E-Car | 25 25 (substrats 60~70) | 95 | 1.0 | 70+25+(3)
Room-air purifier | HEPA | 25~30 30 (substrate 70) | 99.95 | 3.0 | 70+30+(3)
HVAC | Medium 65 85 95 | 15~20 15 20~25 20 25~35 25 (substrate60) | 65 85 95 | 0.6 0.8 1.0 | 60+15+(1~2) 60+20+(2) 60+25+(3)
HEPA | HEPA | wet-laid glass 30 (substrate 50+50) | 99.97 | 10 | 50+30+(5)+50 4 layers

## Slide 29: Various Applications.
미세먼지
세균
물방울
화학물질
공기
소리
Filters
Absorptions
Wipers
Protective
masks
Nano-textile
Water-proof
Vent(for C.P)
quick-dry,absorption
Bio-filter
Medical. Cosmetics
sanitary naphkin
Wound bandage
Sound-proof & insulations
Extreme-environmental materials(Insulation)
Chemical-protective
Military.
Energy-storage
29

## Slide 30: ex2) P.V.A(Collagen) nano fabrics-Patch & film : Water-soluble Electro Blown Spinning

## Slide 31: ex3)Heat-resistant Nano separator for E-Car
Main Property | Present | Target Spec.
Porosity | 30~50% | under 50%
pore size | 0.1~1μm | under 1μm
Thickness | 20μm | 16μm
Heat-resistancy (L.O.I) | 100~150℃ | over 160℃ (over 40)
Puncture Strength (ASTM D 5745) | 10N | over 14N
① Modification tech. of P.V.D.F or P. I polymers (Improvement of morecular weight & durability
② How to make ultra-thin nano-fabrics (under 16um).
(Super-caledering tech.)
③ How to increase the puncture strength) & minimize of deviation.
④ How to make a uniform ceramic coating technology.
how to keep the strength
⑤ How to maintain the electrolyte -absorbency
electrolyte
anode
cathode
separator

## Slide 32: ex4)Gas diffusion layer for Hydrogen Fuel cell based on Carbon nanofiber fabrics
Property | unit | PRESENT |  | Target
 |  | dometic | foreign | 
Porosity | % | 50 | 70 | 70~90
pore size | um | under 2 | 1 | under 1
surface resistance | 오옴/sq | 10 | 10 | under 10
Thickness | um | 100 | 50 | under 50
water repellancy |  |  | 5 degree | over 5 degree
◦ How to make & laminate nano-layers by carbonization & stabilization of PAN polymer.
◦ 2nd ultra-high temp.sintering process after 1st stabilization
◦ Water-repellancy treatment & how to control ultra-thin thickness.(calendering)
◦ How to keep & control low surface resisrance.
◦ How to control uniform
Pore size
◦ How to keep high porosity.

## Slide 33
  Patents of Electro-Spinning
33

## Slide 34
FT ENE Co.ltd –Toptech-Lemon(Multi-nozzle system)
  success on commercial production in 2005(P.U lining)-company sold out
Fibrane( Aerodynamic E-Spinning –LAB)
Success on electro-AES blown spinning in 2012
Mass-production with the biggest capacity
Transfer tec. & patent .
* U.S.A & Japan:
* China :
Elmarco ltd.(Czech : Nano-spider)
  Supply facilities(up to 1.6m)
  Nano-spider technology.
  http://www.elmarco.com
  Newzealand : Revolution Fibers co.
The others
Dupont-Cummins
  Donaldson co.
  H & V co. Etc…..
Woo-Ri MNS
Amo Greentech.
Nam-Yang N.W.F Co.itd
Worldwide Status of Nano-Fiber Tech.
Most Advanced & Commercialized
34

## Slide 35
  • Bio-HEPA Filter
  • Bio-Room Air cleaner (HEPA grade)
  • Bio- Fuel filter
  • Bio-Cabin Filter for E-Car
  • Bio-Liquid Filter
  • Filter Bag for dust- collector (hot gas)
  • Gas turbine filters
  • battery separator for E-Car.
  * Gas diffusion layer for H-Car
  • The others etc…
Bio-Nano Tech. For Air-Filters
35

## Slide 36
  Applications field
36

## Slide 37
  Application field
37

## Slide 38
Nano web Developement:
Essential Parameters in Process Control.
Article | Parameter & Problems!
Material | • Select the proper polymer • Viscosity, Density. • Conductivity, • Surface tension
Process | • Hydrostatic pressure • Electric potential (Voltage) • How to recover expensive solvent • Maximize the productivity
The Others Bio-Turnkey Solution | • Solution temp.• Humidity• Airflow & Velocity • How to minimize of deflection • PLA E-Spinning Turnkey Solution : 1MU$ (Width; 1.6m/min, speed: 20m/min) * PVA E-Spinning Solution:Software:0.5MU$.
38

## Slide 39
Nano Fabrics : Commercialized Status
Company | Brand name | Application | Remarks
F Co. (Germany) | V. | Medium filter, Cabin filter | Electro spinning Polycarbonate (1000~2000nm) since 1970.
D co (USA) | Ultra-web | Medium filter, Gas-turbine filter Liquid filter | Nylon, since 1970
H co (England) | Nanos | HEPA filter, Liquid filter | PP, Technology from Nanofiber Tec., Inc (2000)
Korea |  | High-performance textile, Filters, Energy storage. Waterproof for membrane of Mobile Vent, Medical etc | PLA,PVA,Collagen,Chitosan etc. PVDF,P.U, Nylon 66, PVA, PAN, etc.The highest technics & biggest capacity in the world.
39

## Slide 40: Capacity comparison of each Nano-Process
Articles | AES system (Electro blown spinning system) | D Co. (Multi nozzle) | L Co. & T Co (Multi-nozzle) | M co. (Multu-nozzle)
Productivity | 50~200Kg/day at a line (Nylon) (width:1.6m) | 5.0~7.0Kg/day at a line (pilot production scale) (width:1.0m,Nylon) | 8.0Kg/day(L) & 30Kg(T) At 1 lines (P.U & P.V.D.F) (width: 1.6m) | 10~12.0Kg/day at 1 line (P.U) (width:1.6m)
No.of holes/line | Under 1,000 | 8,000 | 9720(L) & 30,000(T) | 10,000
g/day/hole | 100 over | 0.5 | 0.8(F) & 3(T) | 1.0
Application | Air/Liquid filter Cosmetics.Medical, Battery separator etc.. | Air filter | Filter, Apparel Sanitary napkin | Mask filter energy storage, Apparel
Remarks. | • re-modified AES blown spin system • mass production | • • Low-productivity | • Multi nozzle • No. of nozzles is maximized to overcome The low-productivity | • Filters & Cosmetics.
40

## Slide 41: ex5) Nano Protective Fabrics
Nano-fabrics
Nanoweb
Sheet
Fabric or
Non-woven
Ultra- Thin Textile
or
SMS
Polymer
Solution
Electro
Spinning
Nanoweb
Sheet
Direct A-E/Spinning of the Nano-web on Ultra thin Fabrics
No Bonding & Lamination tech.
Post-treatment
- Special Coating
- Print
- etc.
41

## Slide 42
Articles | Nano-textile (SMS or Woven + nano Web) | Gore-Tex (woven +PTFE Film) | Remarks.
Moisture vapor permeability (g/m2/24h) | 4,000~10,000 | 5,000~10,000 | N/T : no-reduction after washing Gore-Tex : decrease after washing
Water proof (mmH2O) | 10,000 | 10,000 | But, over 4,000 after 3-times washing
Absorption. (mm) | Increase 300% vs. woven | Almost same with woven. | C/Knit : 11/6 → 42/39 (PU) T/Suede : 44/5 → 100/100
Dryness. (g/202.5cm2) | 1.15 | 2.53 | ※ Remained weight of 2-Layer fabric
Warmth. (%) | 22.5 | 17.2 | ※ 3-Layer fabric(+ Lining).
Lightness. (g/m2) | Web : 8~20 | Film + PU | ※ P.U weight 10~20 gsm in Hot melt Bonding.
Functionalities of Nano-Protective Fabrics
42

## Slide 43
 | Moisture-vapor permeability | Water proof | absorption | dryness | warmth | lightness | Remarks. % application.
Nano Textile. | ◎ | ○ | ◎ (inside) | ◎ | ◎ | ◎ | •Excellent MVP, Ab, Dry. • wind-proof jacket with lightness. • Sports/Leisure in climbing. due to excellent Ab. & dryness) • Excellent Comfortness vs.Gore-Tex • Non-Swelling, Not noisy
Gore-Tex, Sympatex | ○ | ◎ | Χ | ○ | △ | △ | • Excellent water-proof. • Excellent the extreme environmental materials. • Excellent wind-proof jacket
※ ◎ : Excellent, ○ : Good, △ : Average, Χ : Bad
Performance of NANO-Protective Fabrics
43

## Slide 44
  Protective & Outdoor Clothes Markets.
44

## Slide 45
Small differences make
big changes !
Thanks for listening !