## Slide 1
How Textile Industry Mingle with NonWovens
 | Prof. HU Jinlian
Department of Biomedical Engineering
Laboratory of Wearable Materials for Healthcare
Hong Kong Convention and Exhibition Center
Hong Kong, 30-31 Oct. 2023

## Slide 2
How Textile Industry Mingle with Non-Woven
 | Prof. HU Jinlian
Department of Biomedical Engineering
Laboratory of Wearable Materials for Healthcare
Hong Kong Convention and Exhibition Center
Hong Kong, 30-31 Oct. 2023

## Slide 3
Nonwovens in Apparel and Textiles
Advantages of Nonwovens
Cost effectiveness of Nonwoven
Versatility of Nonwoven Technologies
History of Nonwovens and electrospinning
Versatility of Electrospun NonWoven
Electrospinning and Applications
Functional Nonwovens in Textiles
Cconclusions
Contents

## Slide 4: Nonwovens in Apparel and Textiles

## Slide 5
Advantages of Nonwovens
Breathable
Absorbent
Liquid repellent
Soft, resilient
Stretchable
Disposable
Cushioning
Filtering
Bacterial barrier and sterility
Continuous web, without yarn structure
Versatility
Lightweight nature
Cost-effectiveness
High productivity

## Slide 6
Bringing Convenience, Happiness and Success---Significant

## Slide 7: Cost effectiveness of Nonwoven

## Slide 8: Cost effectiveness of Nonwoven
Fibre Spinning
Yarn Spinning
Weaving Preparation

## Slide 9
Non-woven: from Polymer to Fabrics
Process is so short and the speed is very high
SS: Production speed up to 450 m/min

## Slide 10
Versatility of NonWoven Technologies

## Slide 11
History of Nonwovens
1920s-
1930s
Chicopee
Manufacturing
Corp developed Viscose rayon
Products, for hygiene uses.
1950s
Freudenberg and DuPont developed enhancing technology in spunbond
1970s
Water-jet technology was developed for surgical gauze
1990s
Bicomponent fibers were developed in meltblown and spunbonded nonwovens
Nano-fibers
Electrospinning

## Slide 12: Versatility of Electrospun NonWoven

## Slide 13
Electrospinning and Applications
Electrospinning

## Slide 14
Wearable Sensing Devices
Advanced Functional Nonwovens in Textiles and Apparel
Functional Filtration Systems
Protective Clothing
Hygiene and Biomedical Textiles
Thermoregulatory textiles
Notes: 10.1007/s40820-023-01028-2
https://doi.org/10.1002/smll.202304705
https://doi.org/10.1021/acsnano.3c02099

## Slide 15: Thermoregulatory Textiles

## Slide 16
Heat transfer pathway between the human body and outer environment as well as adverse physiological responses to variations in core body temperature; Metabolic heat and solar absorption are two heat input mechanisms. Output channels include conduction, convection, radiation, and evaporation.
Body Heat: Input, Output and Pphysiological Responses

## Slide 17
A supramolecular-enhanced membrane (SupraEM) acting as a mid-infrared (MIR) reflector to solve the conundrum of warmth-wearability performance.
Low-emissivity passive heating membrane with warmth retention for Thermoregulatory textiles-Warming
https://doi.org/10.1039/D3MH00768E

## Slide 18: Infrared spectroscopy Spectra
(b) Reflectivity, and
(c) Emissivity of PVDF&PU, PVDF/MXene, PU/MXene, and PVDF&PU/MXene.
(d) Schematic diagram of the heating platform experiment, with the heat transfer direction.
(e) Real-time temperature record of PVDF&PU/MXene at 35 °C.

## Slide 19: Mechanism of SUPRAEMs
The optimized configurations of (a) PVDF/MXene, (b)PU/MXene, and
(c) PVDF&PU/MXene during the process of mutual absorption. SEM images and insert pore size distribution of polymers (d) PVDF, (e) PU, and (f) PVDF&PU.

## Slide 20: Performances of SupraEMs
Water vapor transmission rate
Strain-stress curves
Comparison of the maximum temperature difference and maximum withstanding strength with other reported studies.
EMI curves.
TGA curves
DSC curves. Photograph of the combustion process
PVDF and (PVDF/MXene,
PU and PU/Mxene
PVDF&PU and PVDF&PU/MXene.

## Slide 21: Evaporative/radiative electrospun membrane for personal cooling

## Slide 22
Thermoregulatory textiles：
Single-Layer Janus Fabric with Directional Water Transport for Integrated Personal Cooling Management
10.1007/s42765-022-00200-4
A Janus Nonwovens for directional water transport property and cooling management

## Slide 23: Wearable Electronics

## Slide 24
Directional Moisture-Wicking Electronic Skins for Biomechanical Energy Harvesting and
All-Range Health Sensing
10.1007/s40820-023-01028-2
Wearable devices developed from PVDF electrospun nonwovens, integrating moisture-wicking effect and static signal sensing. It can monitor walking, speaking, pulsing.

## Slide 25
Directional Moisture-Wicking Electronic Skins for Biomechanical Energy Harvesting and All-Range Health Sensing
10.1007/s40820-023-01028-2
Wearable devices developed from PVDF electrospun nonwovens, integrating moisture-wicking effect and static signal sensing. It can monitor walking, speaking, pulsing.

## Slide 26: A Bionic Skin for Health Management Excellent Breathability, In Situ Sensing, and Big Data Analysis

## Slide 27
https://doi.org/10.1002/adma.202306435
Wearable devices developed from PVDF electropunk nonwovens, integrating moisture-wicking effect and static signal sensing. It can monitor walking, speaking, pulsing.
A Bionic Skin for Health Management
Excellent Breathability, In Situ Sensing, and Big Data Analysis

## Slide 28
https://doi.org/10.1002/adma.202306435
Wearable devices developed from PVDF electropunk nonwovens, integrating moisture-wicking effect and static signal sensing. It can monitor walking, speaking, pulsing.
A Bionic Skin for Health Management
Excellent Breathability, In Situ Sensing, and Big Data Analysis

## Slide 29
https://doi.org/10.1016/j.nanoen.2023.108734
A biocompatible and antibacterial all-textile structured triboelectric nanogenerator
for self-powered tactile sensing
Anti-bacterial and self-powering nonwovens

## Slide 30
https://doi.org/10.1016/j.nanoen.2023.108734
A biocompatible and antibacterial all-textile structured triboelectric nanogenerator
for self-powered tactile sensing
Anti-bacterial and self-powering nonwovens

## Slide 31
https://doi.org/10.1016/j.nanoen.2023.108734
A biocompatible and antibacterial all-textile structured triboelectric nanogenerator
for self-powered tactile sensing
Anti-bacterial and self-powering nonwovens

## Slide 32: Functional Filtration System

## Slide 33
Multifunctional face mask with high filtration efficiency and signal-sensing ability.
https://doi.org/10.1021/acsnano.3c02099
An Intelligent Wearable Filtration System for Health Management

## Slide 34
Multifunctional face mask with high filtration efficiency and signal-sensing ability.
https://doi.org/10.1021/acsnano.3c02099
An Intelligent Wearable Filtration System for Health Management

## Slide 35
Protein-Based Face Mask with
High SARS-CoV-2 Neutralization Ability and Breathability
Electrospun protein-based masks for anti-COVID-19 virus.
https://doi.org/10.1002/admt.202300590

## Slide 36: Protective Clothing

## Slide 37
Bioinspired Hierarchical Multi-Protective Membrane for
Extreme Environments via Co-Electrospinning-Electrospray Strategy
https://doi.org/10.1002/smll.202304705
Nonwovens from electrospun and electrospray technologies for protective clothing. It is breathable and fire-retardant.

## Slide 38
Bioinspired Hierarchical Multi-Protective Membrane for
Extreme Environments via Co-Electrospinning-Electrospray Strategy

## Slide 41: Others

## Slide 42
Electrospinning Membranes with Directional Water Transport as
Ecofriendly Dry Facial Masks
Advanced Materials Technologies, DOI: (10.1002/admt.201600015)
Janus facial mask with directional water transport properties.

## Slide 43: A skin-like nanostructured membrane for advanced wound dressing

## Slide 44: A skin-like nanostructured membrane for advanced wound dressing

## Slide 45
Conclusions
Nonwovens are versatile and cost-effective technologies compared with traditional woven and knitted fabrics.
Nonwovens have huge applications in Apparel and textiles
Electrospun nonwovens are becoming feasible and provide huge opportunities
Nonwovens now can be modified with advanced and multiple functions to meet new and challenging textiles and apparel requirements by electrospinning

## Slide 46
Thank you